SPEC NOTE: This specification includes materials and installation procedures for Henry BlueskinVPTM 160, a self-adhering weather resistive air barrier membrane meeting the air barrier requirements of the Massachusetts Energy Code for the building envelope. Henry BlueskinVPTM 160 self-adhesive membrane is used in cavity wall construction to provide a water resistant air barrier membrane yet allows for the passage of water vapor.  Henry BlueskinVPTM 160 in conjunction with Henry Blueskin® self-adhered transition membranes, primer and HE925 BES Sealant at terminations and penetrations meets ASTM E-2357.  This specification should be adapted to suit the requirements of individual projects. It is prepared in CSI Master Format and should be included as a separate section under Division 7 - Thermal and Moisture Protection.

PART 1 - GENERAL

1.01	GENERAL REQUIREMENTS

A.	General Conditions, Supplementary Conditions, Instructions to Bidders and Division One General Requirements shall be read in conjunction with and govern this section.

B.	This Specification shall be read as a whole by all parties concerned.  Each Section may contain more or less than the complete Work of any trade.  The Contractor is solely responsible to make clear to the Subcontractors the extent of their Work.

1.02	DESCRIPTION

A.	Supply labor, materials and equipment to complete the Work as shown on the Drawings and as specified herein to bridge and seal the following air leakage pathways and gaps:

1.	Connections of the walls to the roof air barrier.

2.	Connections of the walls to the foundations.

3.	Seismic and expansion joints.

4.	Openings and penetrations of window and door frames, store front, curtain wall.

5.	Piping, conduit, duct and similar penetrations.

6.	Masonry ties, screws, bolts and similar penetrations.

7.	All other air leakage pathways in the building envelope.

- Materials and installation methods of the primary vapor permeable air barrier membrane system and accessories.

- Materials and installation methods of through-wall flashing membranes.

1.03	PERFORMANCE REQUIREMENTS

A.	Provide an air barrier membrane system constructed to perform as a continuous air barrier, and as a liquid water drainage plane flashed to discharge to the exterior any incidental condensation or water penetration.  Membrane system shall accommodate movements of building materials by providing expansion and control joints as required, with accessory air sealant materials at such locations, changes in substrate, perimeter conditions and penetrations.

1.04	RELATED SECTIONS

- Concrete	Section [03 XX XX]

- Masonry	Section [04 XX XX]

- Gypsum Sheathing	Section [06 XX XX]

- Plywood Sheathing	Section [06 XX XX]

- Insulation	Section [07 XX XX]

- Roofing	Section [07 XX XX]

- Wall Panels	Section [07 XX XX]

- Flashing	Section [07 XX XX]

- Sealants	Section [07 XX XX]

- Door Frames	Section [08 XX XX]

- Window Frames	Section [08 XX XX]

1.05	REFERENCES

A.	The following standards are applicable to this section:

1.	ASTM E2357: Standard Test Method for Determining Air Leakage of Air Barrier Assemblies.

2.	ASTM E2178: Standard Test Method for Air Permeance of Building Materials.

3.	ASTM E283: Standard Test Method for Determining the Rate of Air Leakage Through Exterior Windows, Curtain Walls, and Doors Under Specified Pressure Differences Across the Specimen.

4.	ASTM E96: Water Vapor Transmission of Materials.

5.	ASTM C920: Standard Specification for Elastomeric Joint Sealants.

6.	ASTM C1193: Standard Guide for Use of Joint Sealants.

7.	ASTM E84: Standard Test Method for Surface Burning Characteristics of Building Materials.

8.	NFPA: Class A 0 -25 Flame Spread Index 0 -450 Smoke Developed Index.

9.	ICC-ES AC-38: Acceptance Criteria for Water-Resistive Barriers.

10.	ICC-ES AC188:  Acceptance Criteria for Roof Underlayments.

11.	ICC-ES AC48:  Acceptance Criteria for Roof Underlayment for use in Severe Climates.

12.	AAMA 2400: Standard Practice for Installation of Windows with a Mounting Flange in 		Stud Frame Construction.

13.	ASTM E 2112:  Standard Practice for Installation of Exterior Windows, Doors and Skylights.

14.	AAMA 711-05: Specification for Self Adhering Flashing Used for Installation of Exterior Wall Fenestration Products.

B.	AATCC – American Association of Textile Chemists and Colorists.

1.	Test Method 127 Water Resistance: Hydrostatic Pressure Test.

C.	TAPPI

1.	Test Method T-410; Grams of Paper and Paperboard (Weight per Unit Area).

2.	Test Method T-460; Air Resistance (Gurley Hill Method).

1.06	SUBMITTALS

A.	Submit documentation from an approved independent testing laboratory certifying compliance with a) the air leakage rates of the air barrier membrane assembly, including primary membrane, primer and sealants have been tested to meet ASTM E2357, b) ICC-AC 38, c) Peel adhesion to unprimed plywood and cyclic and elongation per ICC-AC 48, d) Class A flame spread index and smoke development per ASTM E-84.

B.	Submit documentation from an approved independent testing laboratory certifying the air leakage and vapor permeance rates of the air barrier membrane, including primary membrane and transition sheets, exceed the requirements of the Massachusetts Energy Code and in accordance with ASTM E2178.

1.	Test report submittals shall include test results of sustained wind loads and gust load air leakage results.

C.	Submit manufacturers’ current product data sheets for the air barrier membrane system.

1.07	QUALITY ASSURANCE

A.	Submit document stating the applicator of the primary air barrier membranes specified in this section is authorized by the manufacturer as suitable for the execution of the Work.

B.	Perform Work in accordance with manufacturer’s written instructions and this specification.

C.	Maintain one copy of manufacturer’s written instructions on site.

D.	Allow access to Work site by the air barrier membrane manufacturer’s representatives.

E.	Components used shall be sourced from one manufacturer, including sheet membrane, air barrier sealants, primers, mastics, flashings and adhesives.

- Single-Source Responsibility:

1.	Obtain air barrier materials from a single manufacturer regularly engaged in manufacturing the product.

2.	Provide products which comply with all federal, state and local regulations controlling use of volatile organic compounds (VOCs).

1.08	MOCK-UP

A.	Construct mock-up in accordance with Section 01 43 39 – Mock-ups.

B.	Provide mock-up of air barrier materials under provisions of Section 01 33 23 - Shop Drawings, Product Data and Samples.

C.	Where directed by [engineer] [architect] [consultant], construct typical exterior wall panel, 6 foot long by 6 foot wide, incorporating substrate, window frame, attachment of insulation and showing air barrier membrane application details.

D.	Allow 48 hours for inspection of mock-up by [engineer] [architect] [consultant] before proceeding with air barrier work. Mock-up may remain as part of the Work.

E.	Test mock-up for air and water infiltration to conform with Section 01400 - Quality Control, in accordance with ASTM E783 and ASTM E1105.

1.09	PRE-INSTALLATION CONFERENCE

A.	Contractor shall convene [one] week prior to commencing Work of this section, under provisions of Section 01 31 19 – Project Meetings.

B.	Ensure all contractors responsible for creating a continuous plane of air tightness are present.

1.10	DELIVERY, STORAGE AND HANDLING

A.	Refer to current Product MSDS for proper storage and handling.

B.	Deliver materials to the job site in undamaged and original packaging indicating the name of the manufacturer and product.

C.	Store rolled materials on end in original packaging.  Protect rolls from direct sunlight and weather until ready for use.

D.	Store air barrier membranes, adhesives and primers at temperatures of 40 degrees F and rising.

E.	Keep solvent away from open flame or excessive heat.

F.	Wasted Management and Disposal

- Separate and recycle waste materials in accordance with Section [01355 - Waste Management and Disposal], and with the Waste Reduction Work Plan

G.	Contractor to verify compliance for Volatile Organic Compounds (VOC) limitations of products to comply with all federal, state and local regulations controlling use of volatile organic compounds (VOCs).

1.12	COORDINATION

- Ensure continuity of the specified membranes throughout the scope of this section.

1.	Air barrier membrane to include self-adhered air barrier, transition membranes and sealant at penetrations.

2.	Drainage plane to include water resistive barrier and flexible flashings to exterior.

1.13	ALTERNATES

- Submit request for alternates in accordance with Section 01 25 00 – Substitution Procedures.

- Submit requests for alternates a minimum of ten (10) working days prior to bid date

- Alternate submission to include:

1.	Evidence that alternate materials meet or exceed performance characteristics of Product requirements as well as documentation from an approved independent testing laboratory certifying the air leakage rates and vapor permeance rates of the air barrier membranes, including primary membrane and transition sheets meet the requirements of ASTM E 2357, the Massachusetts Energy Code and in accordance with ASTM E2178.

2.	Manufacturer’s complete set of details for air barrier membrane system showing a continuous plane of air tightness throughout the building envelope.

- Acceptable alternates will be confirmed by addendum. Substitute materials not approved in writing prior to bid date shall not be permitted for use on this project.

1.14	WARRANTY

A.	Provide manufacturer’s standard 12-year material warranty for air barrier membrane materials, sealant and flashing membrane.

PART 2 - PRODUCTS

  - MATERIALS

- Air barrier membrane components and accessories must be obtained as a single-source from the membrane manufacturer to ensure total system compatibility and integrity.

      - Acceptable Manufacturer:	Henry Company.

999 N. Sepulveda Blvd Ste 800

El Segundo, CA  90245

(800) 486-1278

Web Site: www.Henry.com

2.02	MEMBRANES (Basis-of-Design)

A.	Primary water resistive air barrier membrane shall be BlueskinVPTM 160 manufactured by Henry; a self-adhering air barrier membrane with an engineered film specifically designed to be water resistant and vapor permeable.  Membrane shall have the following physical properties:

1.	Air leakage: <0.004 CFM/ft2 @ 1.57 lbs/ft2 [<0.02L/s/m2 @ 75Pa] when tested in accordance with ASTM E2178,

2.	Water Vapor Permeance: 29 perms to ASTM E96, Method B,

3.	Tested to ASTM E2357 for Air Leakage of Air Barrier Assemblies,

4.	Resistance to Water Penetration: Pass ICC-ES AC 38

5.	Water Penetration Resistance around Nails: Pass when tested to AAMA 711-05 & ASTM D 1970 modified,

6.	Surface Burning Characteristics: Class A, when tested in accordance with ASTM E84: Flame Spread Rating of 0 and Smoke Development Classification of 105,

7.	Basis Weight: Minimum 160 gm/m2, when tested in accordance with TAPPI Test Method T-410,

8.	Tensile Strength: 40 lbF MD and 29 lbF CD per ASTM D828,

9.	Average Dry Breaking Force: 127 lbF MD, and 91 lbF CD per ASTM D 5034,

10.	Cyclic and Elongation: Pass at 100 cycles, -29 degrees C (-20 degrees F) per ICC-ES AC 48

B.	Self-adhering membrane for window sill pan flashings shall be Blueskin( SA, LT, or HT manufactured by Henry; an SBS modified bitumen, self-adhering sheet membrane which is integrally laminated to a blue polyethylene film. Membrane shall have the following physical properties:

- Membrane Thickness: 0.040 inches (40 mils),

- Low temperature flexibility: -30 degrees F to ASTM D146,

- Elongation: 200% minimum to ASTM D412-modifed,

- Minimum Puncture Resistance 40lbf to ASTM E154,

- Lap Peel Strength 10 lbf/in width to ASTM D903 180° bend,

6.	Auxiliary tested component of ASTM E2357 for Air Leakage of Air Barrier Assemblies

C.	Self-adhering membrane for all window jambs, headers, door openings, inside and outside corners, and other transitions shall be pre-cut BlueskinVPTM 160 manufactured by Henry; a self-adhering sheet air barrier membrane with an engineered film specifically designed to be water resistant and vapor permeable. Membrane shall have the following physical properties:

1.	Air leakage: <0.004 CFM/ft2 @ 1.57 lbs/ft2 [<0.02L/s/m2 @ 75Pa] when tested in accordance with ASTM E2178,

2.	Water Vapor Permeance: 29 perms to ASTM E96, Method B,

3.	Tested to ASTM E2357 for Air Leakage of Air Barrier Assemblies,

4.	Resistance to Water Penetration: Pass ICC-ES AC 38,

5.	Water Penetration Resistance around Nails: Pass when tested to AAMA 711-05 & ASTM D 1970 modified,

6.	Surface Burning Characteristics: Class A, when tested in accordance with ASTM E84: Flame Spread Rating of 0 and Smoke Development Classification of 105,

7.	Basis Weight: Minimum 160 gm/m2, when tested in accordance with TAPPI Test Method T-410,

8.	Tensile Strength: 40 lbF MD and 29 lbF CD per ASTM D828,

9.	Average Dry Breaking Force: 127 lbF MD, and 91 lbF CD per ASTM D 5034,

10.	Cyclic and Elongation: Pass at 100 cycles, -29 degrees C (-20 degrees F) per ICC-ES AC 48

Spec Note: Masonry Flashings are typically specified in Section 04 05 23.16.  Co-ordinate material selection and application with air barrier membrane systems.   Blueskin TWF is specifically designed for flashing details with a stronger film and resistance to flow.

D.	Through-wall flashing membrane (Self-Adhering) shall be Blueskin( TWF manufactured by Henry; an SBS modified bitumen, self-adhering (Yellow) sheet membrane complete with a cross-laminated polyethylene film.  Membrane shall have the following physical properties:

1.	Membrane Thickness: 0.0394 inches (40 mils),

2.	Film Thickness: 4.0 mils,

3.	Flow (ASTM D5147): Pass @ 212 degrees F,

4.	Puncture Resistance: 134 lbf to ASTM E 154,

5.	Tensile Strength (film): 5723 psi ASTM D882,

6.	Tear Resistance: 13lbs. MD to ASTM D1004,

7.	Low temperature flexibility: -22 degrees F to CGSB 37-GP-56M

Spec Note: Acceptable substrates for BlueskinVPTM include DensGlass(, exterior grade gypsum board, plywood, OSB, precast concrete, cast-in place concrete, concrete block, steel, aluminum and galvanized metal.  Best practice guide lines for the application of BlueskinVPTM on clean, dry surfaces of sheathing boards includes the use of adhesive-primers.  Applications of BlueskinVPTM on sheathing board surfaces clean of oil, dust, bulk water or other contaminates that would be detrimental to adhesion of membrane, may not require the use of adhesive-primers.  (See also 3.02 Surface Preparation) If appropriate adhesion is not obtained, condition surfaces with HENRY Blueskin( LVC Adhesive or HENRY Blueskin( Adhesive.

2.03	ADHESIVE PRIMERS

A.	Low VOC adhesive primer for primary self-adhering water resistive air barrier membrane, self-adhering transition membrane and SBS modified bitumen membranes at all temperatures shall be Blueskin( LVC Adhesive as supplied by Henry; a low V.O.C. quick setting rubber based adhesive.  Adhesive Primer shall have the following physical properties:

1.	Color: Blue,

2.	Weight: 7.68 lbs/gal,

3.	Solids by weight: 40%,

4.	Max. V.O.C. <240 grams/liter,

5.	Drying time (initial set): 30 minutes at 50% RH and 70 degrees F

B.	Adhesive Primer for primary self-adhering water resistive air barrier membrane, self-adhering transition membrane and SBS modified bitumen membranes in non-regulated VOC areas, at all temperatures shall be Blueskin( Adhesive manufactured by Henry, a synthetic rubber based adhesive, quick setting, having the following physical properties:

1.	Color: Blue,

2.	Weight: 6 lbs/gal,

3.	Solids by weight: 35%,

4.	Drying time (initial set): 30 minutes

2.04	PENETRATION & TERMINATION SEALANT

A.	Termination Sealant shall be HE925 BES Sealant manufactured by Henry; a moisture cure, medium modulus polymer modified sealing compound having the following physical properties:

        - Compatible with sheet air barrier, roofing and waterproofing membranes and substrate,

        - Complies with Fed. Spec. TT-S-00230C, Type II, Class A,

        - Complies with ASTM C 920, Type S, Grade NS, Class 25,

        - Elongation: 450 – 550%,

        - Remains flexible with aging,

        - Seals construction joints up to 1 inch wide,

6.	Auxiliary tested component of ASTM E2357 for Air Leakage of Air Barrier Assemblies

PART 3 EXECUTION

3.01	EXAMINATION

A.	Verify that surfaces and conditions are ready to accept the Work of this section. Notify [engineer] [architect] [consultant] in writing of any discrepancies.  Commencement of the Work or any parts thereof shall mean acceptance of the prepared substrates.

B.	All surfaces must be sound, dry, clean and free of oil, grease, dirt, excess mortar or other contaminants detrimental to the adhesion of the membranes. Fill voids, gaps and spalled areas in substrate to provide an even plane.  Strike masonry joints full-flush.

C.	Curing compounds or release agents used in concrete construction must be resin based without oil, wax or pigments.

D.	Condition materials to room temperature prior to application to facilitate handling.

3.02	SURFACE PREPARATION

A.	Surfaces must be sound, clean and free of oil, grease, dirt, excess mortar or other contaminants. Fill spalled areas in substrate to provide an even plane.

B.	New concrete should be cured for a minimum of 14 days and must be dry before primer for air barrier membranes are applied.

C.	Ensure all preparatory Work is complete prior to applying primary air barrier membrane.

D.	Mechanical fasteners used to secure sheathing boards or penetrate sheathing boards shall be set flush with sheathing and fastened into solid backing.

E.	Pre-cast and concrete block substrates are required to be primed prior to application of self-adhering water resistive air barrier membrane.

3.03	APPLICATION OF ADHESIVE PRIMER

A.	Required ADHESIVE Primer for SBS Modified Self-adhering Membranes.

1.	For the application of SBS modified self-adhering window sill pan flashings, through-wall flashings and other applications of SBS modified self-adhering transition membranes, the substrate needs to be conditioned with applicable adhesive primer.

2.	Apply adhesive primer at rate recommended by manufacturer to all areas to receive SBS modified self-adhering sheet membrane as indicated on drawings by roller or spray and allow to dry.

3.	For applications of SBS modified self-adhered membranes installed over the primary self-adhered water resistive air barrier membrane, the surface of the primary self-adhered water resistive air barrier membrane must be primed and allowed to cure prior to the placement of the SBS modified self-adhered membrane.

B.	Adhesive Primer for Primary Water Resistive Air Barrier Membrane.

1.	Apply adhesive primer as required depending on substrate type and condition of substrate

2.	Where appropriate surface adhesion can not be achieved, prime substrate with specified primer, at a rate of 200-250 sq ft/gal as per Technical Data Sheet.

3.	All pre-cast concrete and concrete block substrates are required to be primed prior to application of self-adhering water resistive air barrier membrane.

4.	Apply adhesive primer as required on surface of Blueskin VP160 where subsequent Blueskin VP160 membrane will overlap such as selvage edge and end laps

3.04	INSTALLTION OF AIR BARRIER SYSTEM

A.	INSIDE AND OUTSIDE CORNERS

1.	Seal inside and outside corners of sheathing boards with a strip of self-adhering vapor permeable membrane extending a minimum of 3 inches on either side of the corner detail.

a.	For inside corners, pre-treat the corner with a continuous ½ inch bead of termination sealant.

b.	Prime surfaces in an intermittent pattern, at a rate of 200-250 sq ft/gal where appropriate to achieve surface adhesion as per manufacturers’ instructions and allow to dry.

c.	Align and position self-adhering transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inches overlap at all side laps and minimum 3 inches overlap at all end laps of membrane.

d.	Roll all laps and membrane with a counter top roller to ensure seal.

B.	TRANSITION AREAS

1.	Tie-in to structural beams, columns, floor slabs and intermittent floors, parapet curbs, foundation walls, roofing systems and at the interface of dissimilar materials as indicated in drawings with self-adhering water resistive air barrier transition membrane.

a.	Prime surfaces in an intermittent pattern, at a rate of 200-250 sq ft/gal where appropriate to achieve surface adhesion as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering transition membrane, remove protective film and press firmly into place.  Provide minimum 3 inch lap to all substrates.

c.	Ensure minimum 2 inches overlap at all side laps and minimum 3 inches overlap at all end laps of membrane.

d.	Roll all laps and membrane with a counter top roller to ensure seal.

Spec Note: Best construction practice requires window sill details to be waterproofed and flashed prior to the placement of the window assembly.  SBS modified self-adhering membranes provide the flexibility to wrap around the configurations of wall openings and provide the self-sealing properties to guard against leaks by mechanical fastener attachment.

Spec Note: Best construction practice for wood frame construction is to protect the jamb of rough openings with the self-adhering water resistive vapor permeable air barrier membrane to reduce the risk of wood deterioration.  Alternatively, for steel stud frame construction with DensGlass( or gypsum sheathing boards a SBS modified membrane may be used to protect the head and jamb of rough openings.

Spec Note: Specific window manufacturer’s instructions over-ride Henry specifications for window openings. The installer is responsible to resolve any conflicts in the specifications, sequencing, materials or techniques between window manufacturer’s instructions and Henry specifications BEFORE CONSTRUCTION.

C.	WINDOWS AND ROUGH OPENINGS

1.	Place specified SBS modified self-adhering window sill pan flashing membrane across window sills.  Pre-treat inside corners with a bead of termination sealant. Install window sill pan membrane and end dam terminations, seal cuts and terminations with termination sealant.

2.	Wrap jamb of rough openings with specified self-adhering water resistive air barrier transition membrane as detailed.

3.	Extend specified self-adhering water resistive air barrier membrane into rough window openings sufficient to provide a connection to interior vapor retarder.

a.	Prime surfaces in an intermittent pattern, at a rate of 200-250 sq ft/gal where appropriate to achieve surface adhesion as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inches overlap at all side laps and minimum 3 inches overlap at all end laps of membrane.

c.	Roll all laps and membrane with a counter top roller to ensure seal.

D.	THROUGH-WALL FLASHING MEMBRANE

1.	Apply through-wall flashing membrane along the base of masonry veneer walls and over shelf angles as detailed.

a.	Prime surfaces and allow to dry, press membrane firmly into place, over lap minimum 2 inches at all end and side laps.  Promptly roll all laps and membrane to ensure the seal.

b.	Applications shall form a continuous flashing membrane and shall extend up a minimum of 8 inches up the back-up wall.

c.	Seal the top edge of the membrane where it meets the substrate using termination sealant.  Trowel-apply a feathered edge to seal termination to shed water.

d.	Install through-wall flashing membrane 1/2 inch from outside edge of veneer.  Provide “end dam” flashing as detailed.

PRIMARY WATER RESISTIVE AIR BARRIER

1.	Apply self-adhering water resistive air barrier membrane complete and continuous to substrate in a sequential overlapping weatherboard method starting at bottom or base of wall and working up in accordance with manufacturer's recommendations and written instructions.  Stagger all vertical joints.

a.	Cut to manageable sections, align and position self-adhering membrane to substrate, remove top panel of protective release film and press firmly into place.

b.	Ensure alignment, hold membrane in place to avoid wrinkles and sequentially remove remaining panels of protective film and press firmly into place.

c.	Ensure minimum 3 inch overlap at all ends and 2 inch side laps of subsequent membrane applications.

c.	Pressure roll all membrane surfaces, laps and flashings with a counter top roller or ‘J-roller’ to ensure appropriate surface adhesion.

d.	At the end of each days work seal the top edge of the membrane where it meets the substrate with termination sealant.  Trowel-apply a feathered edge to seal termination and shed water.

3.05	APPLICATION OF TERMINATION SEALANT

A.	Seal membrane terminations, heads of mechanical fasteners, masonry tie fasteners, around penetrations, duct work, electrical and other apparatus extending through the primary water resistive air barrier membrane and around the perimeter edge of membrane terminations at window and door frames with specified termination sealant.

B.	Seal the leading edge of membrane terminations and reverse laps.

3.06	FIELD QUALITY CONTROL

A.	Make notification when sections of Work are complete to allow review prior to covering air barrier system.

3.07	PROTECTION

A.	Damp substrates must not be inhibited from drying out.  Drying time varies depending on temperature and relative humidity.  Do not expose the backside of the substrate to moisture or rain.

B.	Cap and protect exposed back-up walls against wet weather conditions during and after application of membrane, including wall openings and construction activity above completed air barrier installations.  Protect air barrier membrane from damage and inclement weather during the construction phase.

C.	Water resistive air barrier membrane is not designed for permanent exposure. Good practice calls for covering as soon as possible, not to exceed 150 days.

D.	Regional weather conditions and daytime sunlight temperatures may require the membrane to be protected under the 150 day exposure limit.

END OF SECTION